In situ resistance measurements and low temperature synthesis of superconducting MgB2 bulk samples

Qing Rong Feng, Xin Wang, Xin-Yie Wang, Guang-cheng xiong

Department of Physics and Mesoscopic Physics National Laboratory, Peking University,

Beijing 100871, P.R. China

Abstract

Superconducting MgB2 bulk samples were simply sintered by heating stoichiometric mixture of Mg and B in vacuum. In situ resistance measurements were performed carefully in order to find the best annealing process. The in situ resistance measurements exhibit a decrease in resistance when the heating temperature is increased. The measurements suggested that the Mg powder melting temperature was below 650℃ and temperature of 800℃ was higher than required. A MgB2 bulk sample sintered at 750℃ has a superconducting transition temper of Tc(R=0)=40.3 K, higher than that sintered at 680 or 810℃.

Published on Solid State Communications, 122(2002), 459-461.