In situ resistance measurement of superconducting MgB2

in flowing argon atmosphere

Qing-rong Feng, Xun Chen, Yu-hao Wang, Xin Wang, Guang-cheng Xiong, Zheng-xiang Gao

Department of Physics and Mesoscopic Physics National Laboratory, Peking University,

Beijing 100871, P.R. China

Abstract

In situ resistance measurement of MgB2 sample was performed in flowing argon atmosphere. This set of measuring curve was compared with the in situ resistance measurement result of MgB2 sample performed in vacuum. This measurement result presents a resistance decreasing taken as a whole as increasing temperature from room temperature to 800℃, and it indicated that the Mg powder began to melt at about 530℃.At this temperature the resistance values of MgB2 sample presented a sharp down, and it is lower than MgB2 sample prepared in vacuum conditions that appeared at 638℃.This indicated that the phase formation of MgB2 in argon atmosphere was at lower temperature than in vacuum.

Published on Physica C, 386(2003), 653-656.