Study of the behavior of the ρ–T curve of YBa2Cu3Oy

during synthesis in ambient air

Qing-rong Feng, Xin-jie Wang, Ke Cao

Department of Physics, Peking University, Beijing 100871, P.R. China

Abstract

The relation of the resistivity vs. synthesizing temperature of YBa2Cu3Oy samples was studied while the material being was prepared under atmospheric conditions. A set of ρ–T curve was obtained for the entire process. At the end of the last sintering step the resistivity values of the YBa2Cu3Oy sample was ρ1233=5.64×10-2 Ω·cm at 960℃, and ρ300=4.32×10-3 Ω·cm at room temperature. The ρ–T curves for the heating stages also show that the formation temperature of YBa2Cu3Oy crystal grains and the re-crystallization temperature are in the range of 480-870℃. When a YBa2Cu3Oy samples was reheated, the ρ–T curve also shown that the orthorhombic-tetragonal phase transformation of YBa2Cu3Oy sample occurred at 690℃.

Published on Physica C, 390(2003), 151-159.