Resistivity-temperature characteristics of sol gel YBa2Cu3Oy samples

synthesized in flowing oxygen atmosphere

Zhou Zeng-Jun(周增均), Zhou Zuo-Wei(周卓为), Zhou Liang-Yu(周良玉), Lin Li(林莉),

Li Xing-Guo(李星国), and Feng Qing-Rong(冯庆荣)

School of Physics and State Key Laboratory of Artificial Microstructure and Mesoscopic Physics,

Peking University, Beijing 100871, China

Department of Chemistry, Peking University, Beijing 100871, China

Abstract

The relation ship of resistivity versus synthesizing temperature of sol gel YBa2Cu3Oy samples was studied while prepared under flowing oxygen conditions. A set of high-temperature ρ–T curves was obtained for the whole process. After the sample finished the test measuring, its resistivity was ρ300=9.83×10-3 Ω·cm at room temperature. The ρ–T curve also showed that the orthorhombic-tetragonal phase transformation of sol-gel YBa2Cu3Oy sample occurred at 581℃ as the sample in the rising temperature process, but at 613℃ in the cooling process, lower than that of the samples made by using the conventional powder metallurgy methods.

Published on Chinese Physics, 13(2004), 1-5.